TECHNICAL DATA SHEET

OneAqua W/B Polyurethane UV Resistance Top Coat

OneAqua 2KU is a two-component water base high solids polyurethane. This product offers a remarkable combination of performance properties not found in other water base polymer coatings. OneAqua 2KU produces protective films which are hard, flexible and very impact resistant. These coatings feature high abrasion and scratch resistance, exterior durability, easy soil release and excellent resistance to a broad range of chemicals. Unlike the Solvent base like OneThane VOC are very low perfect to use under conditions where solvent fumes are not acceptable. OneAqua 2KU has been designed as a high performance top-coat in various protective coating and seamless flooring applications. It provides maximum cleanability and stain resistance when used as a finish coat in color chip flooring. This coating is ideally suited for clean room floors, automotive repair facilities, aircraft hangers, and other high wear areas requiring resistance to fuels and chemicals. CHEMICAL COMPOSITION Water base polyester crosslinked with aliphatic polyisocyanate.

PHYSICAL PROPERTIES

PROPERTIES PERFORMANCE

| Mixing Ratio by Volume | 4:1 Solid |  | Gloss (60 degrees) | 90-95 |
| --- | --- | --- | --- | --- |
| Content by Weight | 60.5% Solids |  | Hardness (Sward) | 30 |
| Content by Volume | 62.5% |  | Pencil Hardness (ASTM D-3363) | F-HTabor |
| Volatile Organic Compounds | 420g/liter |  | Abrasion (1000gm load 1000 cyc, CS-17 wheel) | 60-65mg loss |
| Viscosity CPS (77 Degrees) | 400avg |  | Flexibility (ASTM D-222) | Passes 1/8” |
| Pot Life (77th @ 1qt) | 1,5 min |  | Impact Resistant (ASTM D-2794) | 160in/lb D&R |
| Pot Life (95th @ 1qt) | 1.0 hr |  |  |  |
| Dry to Touch | 2-3 hrs |  |  |  |
| Recoat | 10-12hrs light |  |  |  |
| Traffic | 4-6 hrs |  |  |  |
| Full Cure | 4 days |  |  |  |

CHEMICAL AND STAIN RESISTANCE

| Urine | No Effect |  | 50% Sodium Hydroxide | No Effect 25% |
| --- | --- | --- | --- | --- |
| Blood | No Effect |  | Hydrochloric Acid | No Effect 25% |
| Whiskey | No Effect |  | Acetic Acid | No Effect 25% |
| Black Ink | No Effect |  | Nitric Acid | No Effect |
| Brake Fluid | No Effect |  |  |  |
| Skydrol B-4 | No Effect |  |  |  |
| Hydraulic Fluid #83282 | No Effect |  |  |  |
| Mineral Spirits | Film Softened |  |  |  |
| Xylene | Film Softened |  |  |  |
| MEK | Film Softened |  |  |  |

MOISTURE VAPOR EMISSIONS/ALKALINITY PRECAUTIONS

All interior concrete floors not poured over an affective moisture vapor retarder are subject to possible moisture vapor transmission and related high levels of alkalinity that may lead to blistering and failure of the coating system. It is the coating applicator’s responsibility to conduct calcium chloride and relative humidity probe testing to determine if excessive levels of vapor emissions or alkalinity are present before applying any coatings. These test kits are available from Garage Sealers. Garage Sealers and its agents will not be held responsible for coating failures due to undetected moisture vapor emissions or related high levels of alkalinity.

SURFACE PREPARATION

Oneaqua 2KU is intended t be applied over primed or previously coated surfaces. When properly prepared it can be applied  to concrete. Surface must be absolutely clean, dry and free from all dirt, wax, oil, chalk, incompatible paint or detergent film. Fully cured, previously coated surfaces must be cleaned and sanded lightly with an 80-100 grit sandpaper or otherwise mechanically abraded before recoating. If multiple coats of Oneaqua 2KU are applied, apply additional coats as soon as possible. If more than 24 hours has elapsed or the coating cannot be indented with a fingernail, lightly sand surface to insure inter-coat adhesion.

MIXING INSTRUCTIONS

Mix only that amount of material that can be used in a 2-hour period at 77. Higher temperatures and the addition of accelerator will reduce work time. In hot weather, mix smaller batches. If using the pigmented system, premix part A well before adding Part B. Combining ratio is 4 Part A to 1 Part B. Proportion the amounts carefully and mix for two full minutes. Avoid contamination with moisture. Reseal partially used containers completely.

APPLICATION RECOMMENDATIONS

Oneaqua 2KUkit of 1.25 gal covers aprx 550-650 sq. ft per gallon using a 3/8” or 1/2” nap roller.

HANDLING PRECAUTIONS

Material is combustible. Extinguish all flames, pilot lights and electrical motors until all vapors are gone. The vapor is harmful. Use only with adequate ventilation/or appropriate cartridge type respirator. Avoid contact with skin, wear protective gloves. Read MSDS sheets before using.

SLIP AND FALL

OSHA and the American Disabilities Act (ADA) have now set enforceable standards for slip-resistance on pedestrian surfaces. The current coefficient of friction required by ADA is .6 on level surfaces and .8 on ramps. Garage Sealers recommends the use of angular slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy condition. It is the contractor and end users’ responsibility to provide a flooring system that meets current safety standards. Garage Sealers or its agents will not be responsible for injury incurred in a slip and fall accident.