TECHNICAL DATA SHEET

PHYSICAL PROPERTIES

One Guard 100% Solids Epoxy & Fast Cure

OG Epoxy is low viscosity, 100% solids resin system used in a variety of flooring applications including high build coatings, aggregate-filled flooring and decorative epoxy pebble applications. This material cures blush-free and provides an outstanding balance of physical strength, flexibility and chemical resistance. OG Epoxy has excellent clarity for use over color quartz aggregate and decorative architectural concrete. The pigmented material features high pigment loading for good substrate hide and color consistency when roller applied. OG Epoxy has considerably lower viscosity than most competitive products providing improved handling at cooler temperatures and exceptional troweling characteristics. The lower viscosity allows for the addition of fine silica fillers for easy application of “slurry” type floors. A fast cure hardener is available when cold weather cure down to 40 degrees or accelerated room temperature cure is required. The versatility of OG Epoxy makes it ideal finish coat or aggregate binder in a wide variety of flooring applications including manufacturing facilities, warehouses, correctional facilities, loading docks and other areas requiring high performance flooring. PROPERTIES PERFORMANCE

| Mixing Ratio by Volume | 2:1 Solid |  | Gloss (60 degrees) | 90-95 |
| --- | --- | --- | --- | --- |
| Solid Content | 100% |  | Hardness (Sward) | 30 |
| Content by Volume | 62.5% |  | Pencil Hardness (ASTM D-3363) | F-HTabor |
| Volatile Organic Compounds | 420g/liter |  | Abrasion (1000gm load 1000 cyc, CS-17 wheel) | 60-65mg loss |
| Viscosity CPS (77 Degrees) | 500avg |  | Flexibility (ASTM D-222) | Passes 1/8” |
| Pot Life (77th @ 1qt) | 25min |  | Impact Resistant (ASTM D-2794) | 160in/lb D&R |
| Pot Life (95th @ 1qt) | 17 min |  |  |  |
| Dry to Touch @77’ | 4-6hrs |  |  |  |
| Recoat | 12-16hrs light |  | High temperatures over 77th will speed curing times and reduce pot life. |  |
| Foot Traffic | 8-10hrs |  |  |  |
| Full Cure | 7days |  |  |  |

CHEMICAL AND STAIN RESISTANCE

| Urine | No Effect |  | 50% Sodium Hydroxide | No Effect 25% |
| --- | --- | --- | --- | --- |
| Blood | No Effect |  | Hydrochloric Acid | No Effect 25% |
| Whiskey | No Effect |  | Acetic Acid | No Effect 25% |
| Black Ink | No Effect |  | Nitric Acid | No Effect |
| Brake Fluid | No Effect |  | Vegetable Oil | No Effect |
| Skydrol B-4 | No Effect |  | Gasoline | No Effect |
| Hydraulic Fluid #83282 | No Effect |  | Motor Oil | No effect |
| Mineral Spirits | No Effect |  | Break Fluid | No effect |
| Xylene | Film softening/film recovers |  |  |  |
| MEK | Film Softened |  |  |  |

MOISTURE VAPOR EMISSIONS/ALKALINITY PRECAUTIONS

All interior concrete floors not poured over an affective moisture vapor retarder are subject to possible moisture vapor transmission and related high levels of alkalinity that may lead to blistering and failure of the coating system. It is the coating applicator’s responsibility to conduct calcium chloride and relative humidity probe testing to determine if excessive levels of vapor emissions or alkalinity are present before applying any coatings. These test kits are available from Garage Sealers. Garage Sealers and its agents will not be held responsible for coating failures due to undetected moisture vapor emissions or related high levels of alkalinity.

SURFACE PREPARATION

Concrete must be cured 30 days and be clean, structurally sound, and free of wax, loose paint or curing compounds. However standing water should be removed. Concrete should be shot blasted acid etched or diamond grinded to achieve a minimum of 5 mil profile. If acid etched, use of a floor machine with a nylogrit brush is required. Etched surface must be neutralized with ammonia and water. If surface is prepared by diamond grinding, grind thoroughly to “open up” the surface. Vacuum concrete dust and rinse surface well. Previously coated surfaces must be mechanically cleaned and abraded with steel wool or 80 grit sandpaper. If applied over acid stains, surface must be properly neutralized with ammonia and water.

MIXING INSTRUCTIONS

Mix only that amount of material that can be used. In very hot weather it is advisable to mix smaller batches to ensure good flow and workability. Because color change can occur as mixed material advances into its pot life, when using as a pigmented finish coat, mix only that amount of material that can be used in one hour. Premix Part A before blending with Part B. Combining ratio is 2 Parts A to 1 Part B. Proportion the amounts carefully for two full minutes using a low speed drill, scraping the bottom and sides of the mixing vessel.

APPLICATION RECOMMENDATIONS

Estimate of 500 sq feet coverage per 4.5-gallon kit. if conditions are very cool and/or damp, 48 hours cure time should be allowed before recoating if needed.  When using a pigmented finish coat, keep a “wet edge” and do not attempt to roll over material that has begun to set as a change in color will result.

HANDLING PRECAUTIONS

Use only with adequate ventilation. Appropriate cartridge-type respirator must be used during application in confined areas. Avoid contact with skin; wear protective gloves. Read Material Safety Data Sheet before using.

SLIP AND FALL

OSHA and the American Disabilities Act (ADA) have now set enforceable standards for slip-resistance on pedestrian surfaces. The current coefficient of friction required by ADA is .6 on level surfaces and .8 on ramps. Garage Sealers recommends the use of angular slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy condition. It is the contractor and end users’ responsibility to provide a flooring system that meets current safety standards. Garage Sealers or its agents will not be responsible for injury incurred in a slip and fall accident.