TECHNICAL DATA SHEET

PROPERTIES PERFORMANCE

Crete-Tac Concrete Adhesive

Crete Tac is a medium-low viscosity, 100% solids epoxy resin blended at the point of use with cycloaliphatic amine For temperatures from 40 0 F to 1040 F BENEFITS: - Superior durability e Bonds newly poured concrete to old concrete - Anchors steel bolt and bars to concrete - Superior flexibility and Thermoresistant to high and low temperatures RECOMMENDED USES: Crete Tac was designed as an adhesive for the purpose of bonding newly poured concrete to old and for anchoring steel bolts and bars in concrete; may be used to slip proof" concrete, fill and level chuck holes and spalled areas. PHYSICAL PROPERTIES Crete-Tac has considerably high viscosity than most competitive products providing improved handling at cooler temperatures and exceptional troweling characteristics. The lower viscosity allows for the addition of fine silica fillers for easy application of “slurry” type. A fast cure hardener is available when cold weather cure down to 40 degrees or accelerated room temperature cure is required.

| Mixing Ratio by Volume | 2:1 Solid |  | Gloss (60 degrees) | 90-95 |
| --- | --- | --- | --- | --- |
| Solid Content | 100% |  | Hardness (Sward) | 30 |
| Content by Volume | 62.5% |  | Pencil Hardness (ASTM D-3363) | F-HTabor |
| Volatile Organic Compounds | 420g/liter |  | Abrasion (1000gm load 1000 cyc, CS-17 wheel) | 60-65mg loss |
| Viscosity CPS (77 Degrees) | 1600-1800 avg |  | Flexibility (ASTM D-222) | Passes 1/8” |
| Pot Life (77th @ 1qt) | 20min |  | Impact Resistant (ASTM D-2794) | 160in/lb D&R |
| Pot Life (95th @ 1qt) | 17 min |  | COLOR Clear and also Available tinted |  |
| Dry to Touch @77’ | 4-6hrs |  |  |  |
| Recoat | 12-16hrs light |  | High temperatures over 77th will speed curing times and reduce pot life. |  |
| Foot Traffic | 12 hrs |  |  |  |
| Full Cure | 4 days |  |  |  |

Compressive Strength (ASTM D-695 67T) 9,000 psi Tensile Strength (ASTM D-638 6T) 5,500 psi Bond Strength (ASTM D-4541) 1,020 psi Shore D Hardness (ASTM D-1706) 80

Elongation, Ultimate %10

Water Absorption (24hr) % (ASTM D-570-63)

The data shown above reflects typical results based on laboratory testing under controlled conditions. Reasonable variations from the data shown above may reflect PACKAGING/COVERAGE:

Adhesive coat:	 @ 20-30 mils

COVERAGE: 50 sq. feet per gallon, surface pits will affect coverage rate

PRECAUTIONS:

CHEMICAL AND STAIN RESISTANCE

FOR INDUSTRIAL USE ONLY. Always use protective clothing, gloves and goggles consistent with OSHA regulations during use. Avoid eye and skin contact. Do not ingest or inhale. Refer to Material Safety Data Sheet (MSDS

| Urine | No Effect |  | 50% Sodium Hydroxide | No Effect 25% |
| --- | --- | --- | --- | --- |
| Blood | No Effect |  | Hydrochloric Acid | No Effect 25% |
| Whiskey | No Effect |  | Acetic Acid | No Effect 25% |
| Black Ink | No Effect |  | Nitric Acid | No Effect |
| Brake Fluid | No Effect |  | Vegetable Oil | No Effect |
| Skydrol B-4 | No Effect |  | Gasoline | No Effect |
| Hydraulic Fluid #83282 | No Effect |  | Motor Oil | No effect |
| Mineral Spirits | No Effect |  | Break Fluid | No effect |
| Xylene | Film softening/film recovers |  |  |  |
| MEK | Film Softened |  |  |  |

MOISTURE VAPOR EMISSIONS/ALKALINITY PRECAUTIONS

All interior concrete floors not poured over an affective moisture vapor retarder are subject to possible moisture vapor transmission and related high levels of alkalinity that may lead to blistering and failure of the coating system. It is the coating applicator’s responsibility to conduct calcium chloride and relative humidity probe testing to determine if excessive levels of vapor emissions or alkalinity are present before applying any coatings. These test kits are available from Garage Sealers. Garage Sealers and its agents will not be held responsible for coating failures due to undetected moisture vapor emissions or related high levels of alkalinity.

SURFACE PREPARATION

Apply only to clean, dry and sound concrete substrates that are free of all coatings, sealers, curing compounds, oils, dirt, or greases. Comprehensive Data Sheet available. New concrete should be cured a minimum of 28 days. Concrete that has been contaminated with chemicals or other foreign matter must be neutralized or removed. Remove any laitance or weak surface layers. Concrete should have a

minimum surface tensile strength of 300 psi, as verified by an elcometer test. Surface profile shall be CSP-3 to CSP-5 meeting ICRI (Intonational Concrete Repair Institute) standard guideline #03732 for coating concrete, producing a profile equal to 60-grit sandpaper or coarser. Prepare surface by mechanical means to achieve this desired profile. Moisture vapor transmission should be 3 lbs. or less per 1,000 square feet over a 24 hour time period, as confirmed through a calcium chloride test or other quantative testing methods. All surface irregularities, cracks, expansion joints and control joints should be properly addressed prior to application. Outgassing may occur due to the porosity of some concrete surfaces. To reduce the effect of outgassing, the primer and coating should be applied when the temperature of the concrete substrate is dropping. however, the concrete substrate temperature should be measured with a surface thermometer for verification. Double priming will greatly reduce the effects of outgassing by additionally filling the pores in the concrete. Refer to Co-Polymer NAC Surface Preparation Guidelines for details.

MIXING INSTRUCTIONS

Mix only that amount of material that can be used. In very hot weather it is advisable to mix smaller batches to ensure good flow and workability. Because color change can occur as mixed material advances into its pot life, when using as a pigmented finish coat, mix only that amount of material that can be used in one hour. Premix Part A before blending with Part B. Combining ratio is 2 Parts A to 1 Part B. Proportion the amounts carefully for two full minutes using a low speed drill, scraping the bottom and sides of the mixing vessel.

APPLICATION RECOMMENDATIONS

- Blend two (2) volumes of Crete Tac Resin with one (1) volume of Hardener

Stir with mechanical mixer for a minimum of two (2) minutes.

- For "bonding" of old to new concrete, pour onto the prepared surface and spread with a notched trowel at the rate of 100 sq. ft. per gallon. Apply the new concrete topping before the Crete Tac film gels otherwise failure at the bond line will occur.

- For embedding anchor bolts add three (3) to four (4) volumes of a clean and dry aggregate, silica or masonary sand, to each volume of resin/hardener, blend and stir until the aggregate is uniformly wetted. Partially fill hole, set the bolt and fill with additional material.

- Remove uncured resinous materials from tools. For best results, clean tools and equipment with xylene. Always wear gloves when using this product.

HANDLING PRECAUTIONS

Use only with adequate ventilation. Appropriate cartridge-type respirator must be used during application in confined areas. Avoid contact with skin; wear protective gloves. Read Material Safety Data Sheet before using.

SLIP AND FALL

OSHA and the American Disabilities Act (ADA) have now set enforceable standards for slip-resistance on pedestrian surfaces. The current coefficient of friction required by ADA is .6 on level surfaces and .8 on ramps. Garage Sealers recommends the use of angular slip-resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy condition. It is the contractor and end users’ responsibility to provide a flooring system that meets current safety standards. Garage Sealers or its agents will not be responsible for injury incurred in a slip and fall accident.